sofSURFACES Inc.

4393 Discovery Line

Petrolia, ON  Canada N0N 1R0

Toll Free	(800) 263-2363

Phone	(519) 882-8799

Fax	(519) 882-2697
Website	www.sofsurfaces.com
E-mail	info@sofsurfaces.com

Product Guide Specification

Specifier Notes: This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, contained in the CSI Manual of Practice. The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code. Coordinate this section with other specification sections and the Drawings. Delete all Specifier Notes when editing this section.

SECTION 07761

RUBBER PAVING TILES (duraSTRONG RPT)

Specifier Notes: This section covers sofSURFACES “duraSTRONG” resilient, interlocking pavers used for architectural rooftop applications, ballast, patios, walkways and decks etc. Consult sofSURFACES for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Resilient, interlocking, architectural rubber paving tiles and ballast.

1.2	RELATED SECTIONS

Specifier Notes: Edit the following list of related sections as required for the project. List other sections with work directly related to this section. Include the section number and title of the following Division 7 section. Delete if roof pavers will be installed over an existing roof.

A.	Section 07_______ - _______________ Roofing.

B.	Section 07720 – Rubber Paving Tile Accessories.

1.3	REFERENCES

Specifier Notes: List standards referenced in this section, complete with designations and titles. This article does not require compliance with standards, but is merely a listing of those used.

A.	ASTM C 67 - Standard Test Methods for Sampling and Testing Brick and Structural Clay Tile.

B.	ASTM D 395 - Standard Test Methods for Rubber Property--Compression Set.

C.	ASTM D 412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers--Tension.

D.	ASTM D 573 - Standard Test Method for Rubber-Deterioration in an Air Oven.

E.	 ASTM D 624 - Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers.

F.	ASTM D 1667 - Standard Specification for Flexible Cellular Materials-Vinyl Chloride Polymers and Copolymers (Closed-Cell Foam).

G.	ASTM D 2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Floor Surfaces as Measured by the James Machine.

H.	ASTM D 2859 - Standard Test Method for Ignition Characteristics of Finished Textile Floor Covering Materials.

Specifier Notes: Include ASTM E 108 when specifying duraSTRONG Premium series roof pavers.

I.	ASTM E 108 - Standard Test Methods for Fire Tests of Roof Coverings.

J.	ASTM E 303 - Standard Test Method for Measuring Surface Frictional Properties Using the British Pendulum Tester.

1.4	SUBMITTALS

A.	Comply with Section 01330 - Submittal Procedures.

B.	Product Data:  Submit manufacturer's product data and installation instructions.

C.	Samples:  Submit manufacturer's sample of 1 full paver.

D.	Certificate of Compliance: Submit manufacturer's certificate of compliance indicating materials comply with specified requirements.

E.	Manufacturer's Project References:

1.	Submit list of successfully completed projects.

2.	Include project name and location, name of architect, and type and quantity of duraSTRONG Rubber Paving Tiles furnished.

F.	Installer's Project References:

1.	Submit list of successfully completed projects.

2.	Include project name and location, name of architect, and type and quantity of rubber paving tiles installed.

G.	Maintenance Instructions: Submit manufacturer's maintenance and cleaning instructions.

H.	Warranty:  Submit manufacturer's standard warranty.

1.5	QUALITY ASSURANCE

A.	Manufacturer's Qualifications:  Manufacturer shall meet a minimum of 1 of the following 2 requirements.

1.	Continuously engaged in manufacturing of rubber paving tiles of similar type to that specified, with a minimum of 10 years successful experience.

2.	Furnished a minimum of 1,000,000 square feet of rubber paving tiles of similar type to that specified.

B.		Installer's Qualifications:

1.	Successful experience in installation of rubber paving tiles of similar type to that specified, with a minimum of 10 projects completed within last 5 years.

2.	Employ persons trained for installation of rubber paving tiles.

3.	Approved by manufacturer.

1.6	DELIVERY, STORAGE, AND HANDLING

A.	Delivery: Deliver materials to site in manufacturer's original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.	Storage:

1.	Store materials in accordance with manufacturer's instructions.

2.	duraSTRONG Rubber Paving Tiles:

a.	Store rubber paving tiles in a dry area at a minimum temperature of 50 degrees F (10 degrees C) for a minimum of 72 hours before installation.

b.	Protect rubber paving tiles from direct sunlight before installation.

3.	Adhesive: Store adhesive in a dry area at a minimum temperature of 50 degrees F (10 degrees C).

C.	Handling: Protect materials during handling and installation to prevent damage.

1.7	ENVIRONMENTAL REQUIREMENTS

A.	Rubber Paving Tile Temperature: Ensure surface temperature of rubber paving tiles is a minimum of 40 degrees F (4 degrees C) at time of installation.

B.	Air Temperature: Ensure air temperature is a minimum of 40 degrees F (4 degrees C) for a minimum of 24 hours before and during installation.

1.8	WARRANTY

A.	Materials: duraSTRONG Rubber Paving Tiles shall be warranted for defects in materials for Limited Lifetime from date of completed installation.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	sofSURFACES, 4393 Discovery Line, Petrolia, ON N0N 1R0, Canada.
Toll Free (800) 263-2363
Phone (519) 882-8799
Fax (519) 882-2697
Website www.sofsurfaces.com/durastrong  E-mail info@sofsurfaces.com

2.2	duraSTRONG Rubber Paving Tiles

A.	Roof Pavers:  “duraSTRONG”.

Specifier Notes: Specify Plus or Premium series of duraSTRONG Rubber Paving Tiles. Consult sofSURFACES for assistance in determining required series.

1.	Series: [Plus]  [Premium].

2.	Description: Resilient, interlocking, architectural rubber paving tiles and ballast.

3.	Material: Compression-molded, recycled rubber and binding agents.

4.	Tile Locking: U-shaped male and female configuration on all 4 sides (patented KROSLOCK Tile Locking System) to lock tiles to adjacent tiles.

5.	Top Edges: Chamfered.

6.	Paver Bottom: Hollow core support pedestal pattern. Support pedestals shall have density equivalent to wear layer.

7.	Wear Layer: Compression molded to obtain optimum density and durability.

Specifier Notes: Specify wear layer for Plus or Premium series of duraSTRONG Rubber Paving Tiles.

a.	Plus Series: Elongated rubber buffings and pigment. Minimum 0.375 inch thick.

b.	Premium Series: Virgin TPV rubber. Minimum 0.250 inch thick.

8.	Size: 24 inches by 24 inches, plus or minus 1/8 inch.

Specifier Notes: Specify thickness of rubber paving tiles. Consult sofSURFACES for assistance in determining required thickness.

9.	Thickness:  [2.00 inches]

Specifier Notes: Specify unit weight of the rubber paving tiles based on Plus or Premium series and required thickness.

10.	Unit Weight:

a.	Plus Series:

1)	2.00-Inch Thickness:  6.00 psf.

b.	Premium Series:

1)	2.00-Inch Thickness:  6.00 psf.

11.	Colors:

Specifier Notes: Specify colors for Plus or Premium series of duraSTRONG Rubber Paving Tiles. Any combination of Plus series colors (or Plus series and Premium series colors) can be used to create a speckled appearance. Consult sofSURFACES for availability of custom colors.

a.	Plus Series:  [Basic Black] [Terra Cotta] [Turf Green] [Blue] [Brown] [Gray]               [____________ ]  [As indicated on the Drawings].

b.	Premium Series (customer favorite blends):  [Spring Meadow] [Asphalt] [Sandy Lane] [Multigrain] [Blue Sand] [Roasted Pepper] [Blue Spruce] [Blue Stone] [Coral Clay] [Firebrick] [Green Slate] [Mocha Latte] [Moon Shadow] [Rainforest] [Summer Night] [Sunrise Yellow] [Sunset Orange] etc. [Other: _________________ ]  [As indicated on the Drawings].

Specifier Notes: Specify percent of color in relation to percent of black for Premium series. Must maintain a minimum of 10% black with 90% customizable color. Consult sofSURFACES for additional information. Spring Meadow, Asphalt, Sandy Lane, Multigrain, Blue Sand, Roasted Pepper, Blue Spruce, Blue Stone, Coral Clay, Firebrick, Green Slate, Mocha Latte, Moon Shadow, Rainforest, Summer Night, Sunrise Yellow and Sunset Orange are common customer favorite blends; however, you are able to further customize these color blends or create your own using our online custom color renderer at: http://www.sofsurfaces.com/design-center].

1)	Percent Color:  _______ percent color, _______ percent black.

B.	Test Results:

1.	Freeze Thaw, ASTM C 67: No deterioration.

2.	Rubber Deterioration / Air Oven, ASTM D 573: No deterioration.

3.	Slip Resistance:

a.	ASTM E 303:

1)	Dry:  51.

2)	Wet:  44.

b.	ASTM D 2047:

1)	Plus:  0.533.

2)	Premium:  0.601.

4.	Compression Deflection, ASTM D 1667: 29.5 psi to 25 percent compression.

5.	Compression Set, ASTM D 395: 4.37 percent permanent set.

6.	Tensile Strength, ASTM D 412: 0.636 mpa

7.	Elongation at Break, ASTM D 412: 68.5% Plus 35.3% Premium

8.	Tear Strength, ASTM D 624: 51 (N)

9.	Flammability:

a.	Burning Pill, ASTM D 2859:  Pass.

Specifier Notes: Include the following test result when specifying Plus or Premium Series of Rubber Paving Tiles.

b.	Roof Covering, ASTM E 108: Class A.

2.3	ACCESSORIES

A.	Adhesive:

1.	Single-component, 100 percent solids, polyurethane.

2.	Waterproof.

3.	Tube format.

4.	Approved by manufacturer.

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine areas to receive rubber paving tiles. Notify architect if areas are not acceptable. Do not begin installation until unacceptable conditions have been corrected.

3.2	PREPARATION

Specifier Notes: Due to the porosity of the duraSTRONG Rubber Paving Tiles, it is important that a proper drainage system be constructed.

A.	Prepare sub-surface in accordance with manufacturer's instructions to ensure proper support and drainage for rubber paving tiles.

Specifier Notes: Include the section number of the following Division 7 section for new membrane roofing. Delete the following sentence if roof pavers will be installed over an existing roof.

B.	Sub-surface shall be as specified in Section 07_______ .

C.	Ensure existing sub-surface is clean and sound with no cracks or loose material.

3.3	INSTALLATION

A.	Install rubber paving tiles in accordance with manufacturer's instructions at locations indicated on the Drawings.

B.	 Apply adhesive in accordance with manufacturer's instructions for tile-to-tile
 installation.

C.	Cut rubber paving tiles to fit around fixed obstacles.

D.	Install additional rubber paving tiles securement at perimeter in accordance with manufacturer's instructions.

3.4	CLEANING

A.	Remove adhesive spills from rubber paving tiles in accordance with manufacturer's instructions.

B.	Clean roof pavers in accordance with manufacturer's instructions.

3.5	PROTECTION

A.	Protect completed rubber paving tile surface from damage during construction.

END OF SECTION